## Slide 1: FAA/GMU Project Development of AL MAT224 Dataset (V2.0)
AWG Annual Meeting
03/15/2018

## Slide 2: Introduction – Revision Need
The previously released set of *MAT224 input parameters for Al-2024 did not produce accurate predictions for all six available sets of ballistic impact data
Since the original material model was released, additional mechanical property data has been created by OSU
  High rate Split-Hopkinson Bar tests, with full field strains measured by DIC, and temperature rise measured by high-rate thermal imaging
    We have become convinced that high rate data without DIC is misleading at best, and at worst, dangerous
  Testing to higher rates
  Failure strains at important, previously unmeasured states of stress, using newly designed test specimens
Therefore, it was appropriate to revise the FAA sponsored Al-2024 material model

## Slide 3: AL MAT224 Dataset
6 curves or tables
  LCK1– Hardening curves vs. Strain Rate
  LCKT – Hardening curves vs. Temperature
  LCF – Failure surface vs. Triaxiality & Lode parameter
  LCG – Failure strain scale factor vs. Strain Rate
  LCH – Failure strain scale factor vs. Temperature
  LCI – Failure strain scale factor vs. Element Size (Regularization)
  Beta - Fraction of plastic work converted into heat

## Slide 4: Temperature Series
5 temperatures
  T5=186K, T1=300K, T2=420K, T3=573K and T4=726K

## Slide 5: LCKT
LCKT are scaled down by the factor of SR2/SR3
  Temperature series was conducted at SR3 (strain rate)

## Slide 6: LCK1 (Quasi-static)
LCK1 (Quasi-static) is the same as T1(300K) of LCKT

## Slide 7: LCK1
Nominal strain rate shown below, but test was not isorate
β=0.4

## Slide 8: LCK1 (cont.)
Greater scatter at these highest, non-constant, rate tests
Force levels of simulations are within +/-10% error ranges of tests
SR6 SR7

## Slide 9: LCK1: Strain
SR4_N12 SR5_N1
SR6_N4 SR7_N6

## Slide 10: LCK1: Temperature (K)
SR4_N12 SR5_N1
SR6_N4 SR7_N6

## Slide 11: LCK1: Compression Rate Series
Compression | Strain rate
SR1 | 0.0001
SR2 | 0.01
SR3 | 1.0
SR4 | 1400
SR5 | 4500
SR6 | 7690
SR7 | 9271
SR8 | 10328
Tension and compression behavior is relatively symmetric

## Slide 12: Failure Test Series
 |  | Tri |  |  | Lode angle |  |  | Epf |  | 
 |  | low | high | avg | low | high | avg | low | high | avg
Plane stress series | 1 | -0.36 | -0.40 | -0.38 | 1.00 | 1.00 | 1.00 | 0.21 | 0.30 | 0.25
 | 2 | -0.48 | -0.52 | -0.50 | 0.91 | 0.91 | 0.91 | 0.24 | 0.30 | 0.27
 | 3 | -0.55 | -0.56 | -0.56 | 0.62 | 0.62 | 0.62 | 0.23 | 0.26 | 0.25
 | 4 |  |  |  |  |  |  |  |  | 
Axi-symmetric series | 5 | -0.34 | -0.53 | -0.43 | 1.00 | 1.00 | 1.00 | 0.16 | 0.43 | 0.29
 | 6 | -0.60 | -0.64 | -0.62 | 1.00 | 1.00 | 1.00 | 0.27 | 0.34 | 0.30
 | 7 | -0.67 | -0.68 | -0.67 | 1.00 | 1.00 | 1.00 | 0.28 | 0.29 | 0.29
 | 8 | -0.73 | -0.75 | -0.74 | 1.00 | 1.00 | 1.00 | 0.26 | 0.28 | 0.27
 | 9 | -0.78 | -0.80 | -0.79 | 1.00 | 1.00 | 1.00 | 0.22 | 0.25 | 0.24
 | 10 | -0.88 | -0.90 | -0.89 | 1.00 | 1.00 | 1.00 | 0.20 | 0.22 | 0.21
Plane strain series | 11 | -0.57 | -0.57 | -0.57 | 0.17 | 0.17 | 0.17 | 0.17 | 0.18 | 0.18
 | 12 | -0.65 | -0.66 | -0.66 | 0.08 | 0.08 | 0.08 | 0.19 | 0.22 | 0.20
 | 13 | -0.76 | -0.77 | -0.77 | 0.01 | 0.01 | 0.01 | 0.21 | 0.23 | 0.22
Compression | 14 |  |  |  |  |  |  |  |  | 
Pure shear | 15 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.12 | 0.20 | 0.16
Tension-Shear series | 16 | -0.39 | -0.40 | -0.40 | 0.97 | 0.97 | 0.97 | 0.24 | 0.27 | 0.25
 | 17 | -0.17 | -0.17 | -0.17 | 0.64 | 0.64 | 0.64 | 0.20 | 0.24 | 0.22
New backed punch test series | Unbacked |  |  | -0.65 |  |  | -1.00 |  |  | 
 | Thin |  |  | -0.10 |  |  | -0.75 |  |  | 
 | Thick |  |  | 0.40 |  |  | -0.75 |  |  | 
Compression-shear series | 21 | 0.21 | 0.21 | 0.21 | -0.78 | -0.78 | -0.78 | 0.44 | 0.44 | 0.44
 | 22 | 0.51 | 0.50 | 0.50 | -0.99 | -0.99 | -0.99 | 0.39 | 0.33 | 0.36
Unbacked
Backed
Thin
Backed
Thick
The triaxiality and Lode Parameter of these (or any) tests is never absolutely constant!

## Slide 13: LCF
Quasi-static failure surface

## Slide 14: Plane Stress Series
Dogbone tension with varying notches (Case 01, no notch)

## Slide 15: Axi-Symmetric Series
Circular tension with varying notches (Case 05, no notch)

## Slide 16: Axi-Symmetric Series (cont.)
Circular tension with varying notches

## Slide 17: Plane Strain Series
Thick tension with varying notches (Case 11, no notch)

## Slide 18: Pure Shear
Torsion

## Slide 19: Tension-Shear Series
Axisymmetric, combined tension and torsion

## Slide 20: Compression-Shear Series
Axisymmetric, combined compression and torsion

## Slide 21: New OSU Punch Tests
Designed for Lode Parameter =-1 states of stress
These states of stress are common in ballistic impact, but are difficult to achieve in mechanical property tests
R0.8128mm

## Slide 22: New Punch Tests: FE Model
Quarter symmetric model
Element size at impact area
  0.15 mm (average)
Number of elements through AL plate thickness
  Unbacked (t=1.27 mm): 8 elements
  Backed (t=0.635 mm): 4 elements
Quasi-static analysis
  No rate and temp. curves in MAT224-AL

## Slide 23: New Punch Tests: *CONSTRAINED_TIED_NODES_FAILURE
Element erosion lead to loss of load path
To prevent element erosion
  Applied to two backed tests

## Slide 24: New Punch Tests (cont.)
Unbacked test is approximately in bi-axial tension

## Slide 25: LCG
Element erosion scaling, as function of strain rate
Try05

## Slide 26: LCH
Scaling of element erosion as a function of temperature
 |  | Failure strain |  |  | Scale factor |  | 
SR3 | Temp. (K) | lower | upper | average | lower | upper | average
T5: 186K | 168 | 0.32 | 0.38 | 0.35 | 1.45 | 1.36 | 1.41
T1: 300K | 300 | 0.22 | 0.28 | 0.25 | 1.00 | 1.00 | 1.00
T2: 420K | 420 | 0.23 | 0.63 | 0.43 | 1.05 | 2.25 | 1.65
T3: 573K | 573 | 1.16 | 1.24 | 1.2 | 4.43 | 5.27 | 4.85
T4: 726K | 726 | 2.2 | 3.08 | 2.64 | 10.00 | 11.00 | 10.50

## Slide 27: LCI
Case 01
Case 10
Case 11
Case 15
Case 21
Case 22
Scaling of erosion by element size
Variations due to differences in localization
Lode-dependent regularization
  Mostly independent of Triaxiality
Lode = 1.0
Lode = 0.0
Lode = -1.0

## Slide 28: LCI: Case 01 & Case 10
w/o Reg.
w/ Reg.
w/o Reg.
w/ Reg.
Plane Stress
Axisymmetric

## Slide 29: Case 11 & Case 15
w/o Reg.
w/o Reg.
w/ Reg.
w/ Reg.
Plane Strain
Pure Shear

## Slide 30: LCI: Case 21 – Compression Torsion
w/o Reg.
w/ Reg.

## Slide 31: LCI: Case 22 – Compression Torsion
w/o Reg.
w/ Reg.

## Slide 32: Ball Impact Test - U.C. Berkeley
Plate
  Aluminum 2024-T3
  Dimension: 12-inch by 12-inch square
  3 thicknesses
    0.0623 (1/16) inch
    0.125 (1/8) inch
    0.25 (1/4) inch
Ball
  ½-inch-diameter chrome steel sphere
  Mass: 0.29 oz. (= 0.018125 lbf = 8.3 gram)

## Slide 33: Cylinder Impact Test – NASA GRC
Plate
  Aluminum 2024-T3
  Dimension: 10-inch-diameter circle
  3 thicknesses
    Plate1: 0.125 (1/8) inch
    Plate2: 0.25 (1/4) inch
    Plate3: 0.5 (1/2) inch
Cylinder
  ½-inch-diameter Titanium & Steel cylinders
  Mass (varied cylinder lengths for different masses)
    9.9 gram for Plate1 (Titanium cylinder)
    12.8 gram for Plate2 (Titanium cylinder)
    28.0 gram for Plate3 (Steel cylinder)

## Slide 34: Impact Test Simulations
Sphere
Cylinder

## Slide 35: Sphere Impact (cont.)
MAT224 Dataset (V2.0)
AR-07/26
Johnson Cook Material Model and Results from 2007 FAA Report

## Slide 36: Summary
Al-2024 MAT224 Dataset (V2.0) is essentially complete
FAA will perform checkout of the model
Documentation will be completed
Model demonstrates good predication capability for a variety of ballistic impact tests
  Varying plate thicknesses, velocities, projectile shapes and materials
Qualifications and considerations:
  Very high strain rates required extrapolation of high rate behavior
  Limited correlation of the failure surface in compression was required
    Three failure strains with positive triaxiality is a big improvement over what was previously available
    For V1.0 no failure strains with positive triaxiality were available
    However, three failure strain values does not define the complete positive triaxiality region of the failure surface!

## Slide 37
Thanks