## Slide 1: Material Modeling Unit Systems Verification Inconel-718 V1.2, with Adiabatic Shear Band Capability
Stefano Dolci, Kelly Carney, Paul DuBois, Steve Kan

## Slide 2: V1.2
Test/ simulation: |  |  |  | DBxxx | DB266 | DB271 | DB271
Mesh [mm] plate/proj (proj mat) | tabulated TQC thresholds |  |  | Impact/exit vel. |  |  | 
 |  | [] |  | 220/xx [m/s] 100% pen | 203.8/52.5 [m/s] Highest vel. | 189/0 [m/s] | 161/0 [m/s] 100% contained
0.2/0.2 (A2) | 0.21 | 8000 | 15 | 61.0 | 36.7 | -25.4 | -29.9
0.2/0.2 (A2high) | 0.21 | 8000 | 15 | 61.5 | 40.0 | -22.6 1/2p | -30.1
0.4/0.2 (A2) | 0.19 | 8000 | 20 | 63.5 | 35.4 | -24.1 | -29.3
0.8/0.2 (A2) | 0.14 | 8000 | 26 | 55.1 | 38.8 | -24 | -29.4
1.6/0.2 (A2) | 0.13 | 8000 | 62 | 42.7 | 39.6 | -29.4 | -30.1
1.6/02 (A2high) | 0.13 | 8000 | 62 | 60.5 | 49.7 | -28.1 | -30.3
1.6/1.6 (A2) | 0.13 | 8000 | 62 | 67.1 | 49.1 | -20.6 | -30.6
Test/ simulation: |  |  |  | DBxxx | DB266 | DB271 | DB271
Mesh [mm] plate/proj (proj mat) | tabulated TQC thresholds |  |  | Impact/exit vel. |  |  | 
 |  |  |  | 220/xx [m/s] 100% pen | 203.8/52.5 [m/s] Highest vel. | 189/0 [m/s] | 161/0 [m/s] 100% contained
0.2/0.2 (A2) | 0.21 | 8000 | 15 | 61.0 | 36.7 | -25.4 | -29.9
0.2/0.2 (A2high) | 0.21 | 8000 | 15 | 61.5 | 40.0 | -22.6 1/2p | -30.1
0.4/0.2 (A2) | 0.19 | 8000 | 20 | 63.5 | 35.4 | -24.1 | -29.3
0.8/0.2 (A2) | 0.14 | 8000 | 26 | 55.1 | 38.8 | -24 | -29.4
1.6/0.2 (A2) | 0.13 | 8000 | 62 | 42.7 | 39.6 | -29.4 | -30.1
1.6/02 (A2high) | 0.13 | 8000 | 62 | 60.5 | 49.7 | -28.1 | -30.3
1.6/1.6 (A2) | 0.13 | 8000 | 62 | 67.1 | 49.1 | -20.6 | -30.6

## Slide 3
SI1 vs SI2 vs US blocks scaled tension,
Stress vs Strain
BLOCKS: 1 2
BLOCKS: 3 4

## Slide 4
SI1 vs SI2 vs US blocks scaled tension, max Shear vs Beta
BLOCKS: 1 2
BLOCKS: 3 4

## Slide 5
New SI1 vs SI2 vs US blocks scaled tension, SR vs Beta
BLOCKS: 1 2
BLOCKS: 3 4

## Slide 6
New SI1 vs SI2 vs US blocks scaled shear, Stress vs Strain
BLOCKS: 1 2
BLOCKS: 3 4

## Slide 7
New SI1 vs SI2 vs US blocks scaled shear, max Shear vs Beta
BLOCKS: 1 2
BLOCKS: 3 4

## Slide 8
New SI1 vs SI2 vs US blocks scaled shear, SR vs Beta
BLOCKS: 1 2
BLOCKS: 3 4

## Slide 9: Thank You
Questions?